PaperStone surfaces are slabs made from paper, resin and pigment.  For most of the PaperStone products, the paper component is 100% recycled.  PaperStone surfaces are fabricated much like solid surfaces and can be used for kitchen and bath surfaces, work surfaces, commercial surfaces, table tops, and more.

This Guide 3-Part Specification is ready to be edited according to your project requirements.  To request samples, product literature, or additional assistance, email us at mike@paperstoneproducts.com or call at 360-742-2826, or visit our website www.paperstoneproducts.com

SECTION 12 36 71 – Paper-Composite Countertops

PART 1: GENERAL

  - Section includes:

- Countertops

- Bathroom vanities

- Tabletops

- Conference tables

- Transaction tops

- Reception areas

- Window sills

- Baseboards

- Other applications as shown on drawings

1.2 Related Sections

- Section 12 36 23.13 Plastic-Laminate-Clad Countertops

- Section 12 36 53 Laboratory Countertops

- Section 06 83 13 Resin Composite Paneling

  - References

- ASTM E84 Standard Test Method for Surface Burning Characteristics of Building Materials

- ASTM D527 – Tensile Strength, Tensile Modulus, Elongation

- ASTM D790 – Flexural Strength, Flexural Modulus

- ASTM D696 – Thermal Expansion

- NEMA LD3 Boiling Water Surface Resistance

- NEMA LD3 High Temperature Resistance

- NEMA LD3 Ball Drop (Impact)

- NEMA KD3 Gloss 60 Degree Gardner

- ASTM D785 – Hardness Test

- ASTM D256 – Izod Impact

- ANSI Z124 Abrasion Resistance

- ASTM D570 Water Absorption

- ANSI Z124 Colorfastness

- ASTM D695 Compressive Strength

- NSF/ANSI 51 Food Equipment Materials

- Forest Stewardship Councel (FSC-US), Information regarding FSC in LEED projects

- LEED (Leadership in Energy and Environmental Design green building rating system

  - Submittals

- See Section 01 30 00 – Administrative Requirements, for submittal procedures.

- Product Data: Manufacturer’s data sheets on each product to be used (http://paperstoneproducts.com/information-landing.php), including:

- Product description

- Fabrication/Installation instructions and recommendations

- Storage and handling requirements and recommendations

- Care and maintenance data

- Specimen warranty

- MSDS for finish sealer

- Shop Drawings:

- Indicate color, thickness, and finish

- Indicate field-verified dimensions

- Indicate locations and dimensions of cutouts

- Selection and verification samples:  obtain product samples from manufacturer or distributor in 3.5”x3.5”x.25” or 12”x12”x.75” as needed.

- LEED Report:

- Credit MR 4: Clearly define the percentage of pre-consumer or post-consumer recycled content, percentage of recycled content, product cost per unit, and volume of product must be specified.

- Credit MR 7:  Submittal must prove that qualifying wood based materials (certified by a recognized forest certification scheme) contribute value to the “50% base on cost” threshold related to the percent of Benchmark credit with which the certification scheme is compliant.

- IEQ Credit 4.4:  Submit documentation for paper products made without urea formaldehyde; certify that this contains no added urea-formaldehyde resins.

- ID Credit 1: Innovation in Design.  This credit can be awarded for exceptional performance above the standard LEED requirements set by the Green Building Rating System and/or innovative performance in green building categories.

- Installation Instructions:  Manufacturer’s installation instructions and recommendations/guidelines (http://paperstoneproducts.com/information-landing.php).

- Maintenance Instructions:  Manufacturer’s instructions and recommendations/guidelines for maintaining the surface (http://paperstoneproducts.com/information-landing.php).

  - Quality Assurance

Fabricator Qualifications: fabricator recommended by material manufacturer and/or distributor.

- Installer Qualifications: Fabricator or installer experienced with PaperStone.

  - Delivery, Storage, and Handling

- Remove banding and inspect material immediately upon receipt or at time of will-call.

- Replace all packaging materials with the exception of the banding.

- Store horizontally in a fully supportive manner (Do not store vertically on edge)

- Do not over stack

- Store between 50 and 80 degrees Fahrenheit

PART 2: PRODUCTS

Specifier: make selections where more than one choice is listed below

2.1  Manufacturers

- Approved Manufacturer:  Little Green, LLC dba Paneltech 2999 John Stevens Way, Hoquiam,     WA 98550. Telephone: (360) 538-1480. Web: www.paperstoneproducts.com.

- Substitutions

  - Request for substitutions will be considered in accordance with provisions of Section 01600 – Product Requirements or

  - Substitutions:  Not permitted

2.2 Countertop Assemblies

A.   Countertop Assemblies:  Surfaced with paper composite panel.

  - Thickness

    - Flat Panel Thickness: 3/4" (19mm), minimum or

    - Flat Panel Thickness: _____” (_____mm), minimum.

  - Sinks and Bowls

    - Separate units for over-counter mounting or

    - Separate units for under-counter mounting.

  - Cutouts and Drain Grooves: As shown on drawings.

  - Finish on Exposed Surfaces

    - Matte with field-applied surface sealer.

    - Semi-gloss with field-applied surface sealer.

  - Color: ___________.

  - Exposed Edge Treatment

    - Same thickness as countertop.

    - [Square edge][Radiused edge][Bullnose edge][Ogee edge] [____________]

  - Back and End Splashes:

  - Same panel material as countertops or ___________________.

  - Thickness same as countertops or __________ (1” maximum thickness).

  - Top Profile same as countertop or ______________.

  - Height: __________” (________mm).

  - Color: same as countertop or _______________.

  - Built-up Edges and/or Aprons/Skirts:

    - Build up edge to : __________”

    - Preferred method is a “stacked built-up edge” as per manufacturer’s fabrication guidelines.

2.3  Material

A.  Approved Products:  PaperStone as manufactured by Little Green, LLC dba Paneltech.

B.  Composition: Recycled paper composite panel product that is produced with a proprietary resin which contains no petroleum based ingredients; color consistent throughout thickness.

C.  Size and Weight:

    - Panel size:  Standard sizes are 5’x8’, 5’x10’, 5’x12’, 2.5’x8’, 2.5’x10’, 2.5’x12’

    - Weight: Material weighs 1.8 lbs per square foot of each ¼” of thickness (¼” = 1.8lbs/sq.ft., ½” = 3.6lbs./sq.ft.).

    - Thickness:  Ranges from 1/8” to 1 ¼”.

D.  Properties

  - ASTM E84 Surface burning characteristics: Flame spread index 20, smoke developed index 110.

  - ASTM D2583 Barcol hardness average 60-61

  - ASTM D638 Tensile modulus psi 765,850 and elongation .3%

  - ASTM D790 Flexural strength psi 14,200 and flexural modulus psi 680,350

  - ASTM D696 Thermal expansion 1.92x10-4

  - ASTM D4060/ANSI Z124 abrasion resistance

| No of Cycles | Weight Loss | Thickness Loss |
| --- | --- | --- |
| 500 | .015g | .0015” |
| 1000 | .040g | .0010” |
| 5000 | .530g | .0035” |

  - NEMA LD3 Boiling water resistance rating – no effect – no change in color or surface finish

  - NEMA LD3 High temperature resistance – heated to 365°F then held at 356°F for 20 minutes – slight effect – a change in color or surface finish only visible at certain angles or directions.

  - ASTM D256 Izod impact – a 1.5” steel ball dropped from a height of 2’-6’.  Fracture occurred at 5’5”.

  - ASTM D570 Water absorption – average absorption .251%

  - ASTM D2565 Colorfastness and aging – 200 hours in weatherometer caused no cracking, crazing, blistering or significant change in color or surface texture

  - ASTM D695 Compressive strength average 27,576 PSI

E.  Adhesives

- Touchstone Express II Adhesive by Bonstone is a two-part epoxy especially formulated to bond PaperStone®

F.  Joint Sealant

- Sealant type: Mildew-resistant Silicone

- Sealant color: Clear or White

G. Coating/Sealant – see 2.4F

2.4  Fabrication

- Inspect material for defects prior to fabrication.

- Ensure that the material is within manufacturer’s flatness tolerance.

- Visually inspect material to ensure that an acceptable color match is achieved.

- Record panel number[s] of all material for warranty purposes.

    - Fabricate in accordance to manufacturer’s recommendations/guidelines.  Material can be fabricated ‘dry’ in a similar manner as a traditional wood product, or ‘wet’ in a similar manner as traditional stone.  Manufacturer’s Fabrication Guide clearly explains the unique differences.

    - Layout:  Fabricate tops and splashes in a manner that utilizes the largest panel sizes available, thus minimizing the number of necessary seams.

- Where seams are necessary, ensure they are performed as per manufacturer’s recommendations.  Improper seaming practices can result in structural and/or cosmetic failures.

- Seam placement and planning can be critical.

  - Most colors contain a level of “mottling” which offers a subtle grain direction running lengthwise within the panels.

  - Seams should be at natural position such as corners and midpoints as indicated in drawings.

    - Cutouts: Prepare all cutouts accurately to size.  All exposed edges should be finished/polished.

    - Built-up Edges/Aprons:

    - “Stacked” edges are preferred from both a structural and aesthetic standpoint.

    - “Mitered” edges require additional support and attention to ensure desired aesthetic appearance.

- Sealing/Finishing:

    - Interior Horizontal applications – 2 coats of Osmo Top Oil, maintained with Original Bee’s Wax.

    - Interior Vertical applications – PaperStone Finish, maintained with PaperStone Cleaner/Rejuvenator.

    - Exterior applications -- PaperStone Finish, maintained with PaperStone Cleaner/Rejuvenator.

PART 3: EXECUTION

3.1  Examination

A.  Ensure support structure and/or substrates are prepared properly.

B.  If substrate preparation is the responsibility of another installer, notify [Architect] [____________________________] of unsatisfactory preparation before proceeding.

3.2  Preparation

- Clean surfaces thoroughly prior to installation.

- Prepare surfaces using manufacturer’s recommendations.

- Protect jobsite and surfaces against dust and water.

3.3  Installation

- Position materials to verify correct dimensions and layout.

- Make necessary adjustments.

- Securely attach countertops to cabinets/support structure using concealed fasteners.  Ensure surfaces are level; use of shims may be necessary.

- Seal joints between backsplashes and/or side splashes with recommended sealant.

- Apply appropriate sealer/finish (see 2.4F)

3.4  Cleaning and Protection

  - Clean countertop surfaces thoroughly.

  - Ensure that countertops are sufficiently protected until completion of the project.

  - Touch-up, repair, or replace damaged materials in a satisfactory manner.

  - Apply maintenance product (see 2.4F) and polish.

End of Section